- All dimensions are in inches.

- Material:

  - Substrate:  ROGERS 4003C, .008 thick

  - Met1 and Met2:  0.5 oz. copper per layer

  - Solder mask:  Taiyo PSR-4000, top side only where indicated (Black)

  - Silkscreen:  White

- Unless specified otherwise, tolerances are:

  - PCB outline	± .002

  - Position of internal cutout relative to hole pattern “A” (DIA=.070) is ± .002.

- Burrs shall not exceed .002.

- Copper is pulled back .002 on Met1 and Met2 from edge of PCB.

- Met1 (top metal) features to be within .001 of CAD data base.

- All vias to be located within ± .0015 of CAD data base.

- Fabricate in accordance with IPC-6018B, per IPC-6011 Class 3.

- Bag and tag parts separately.

- All vias to be plated to .0007 min thickness.

- Finished Met1 and Met2 Cu thickness to be .0014 ± .0008.

- Maximum allowable negative feature .0008. Maximum allowable positive feature .0003

- Drill Information

  - DIA = .070 ± .0015, finished size, not plated (hole pattern A)

  - DIA = .125 ± .003, finished size, not plated

  - DIA = .096 ± .003, finished size, not plated

  - DIA = .020 ± .003, drill size, Plated Thru

  - DIA = .012 ± .003, drill size, Plated Thru

  - DIA = .008 ± .003, drill size, Plated Thru

- Plating:

  - Met1 and Met2: Nickel Plate per QQ-N-290, Class 1, Grade G, 200 uin min (5 um min); Gold Plate per ASTM B 488, Type III, Grade A, 3-10 uin (0.08-0.25 um)

- Hole Pattern “A” definition